## Slide 1: Overall Organization
CRIPT End-to-End Test Papers
Calabrese et al. Rubber Recycling
Composition Analysis
Reference to Calabrese et al.
Model Rubber Preparation
SCA Preparation
Laminate Adhesion Strength
Factorial Design with Controls
Analysis of Factorial Design
Recycled Rubbers
Rubber Formulation Ingredients

## Slide 2: Composition Analysis
Vulcanizing fluid 760 (cement)
Lyophilization
Liquid nitrogen
Vulcanizing fluid 760 solids fraction
Vulc Fluid GPC
CHNS
Cushion Gum
TGA
Composition Analysis

## Slide 3: Preparation of Model Rubber
Stearic acid
Carbon black N330
F3 compounding
PBD GPC
High-cis polybutadiene
F3 masterbatch
Zinc oxide
BHT
TBBS
sulfur
F3 uncured
F3 cured
F3 GRP
F3 compound with cure pkg
F3 vulcanization
F3 grinding
Model Rubber Preparation

## Slide 4: Preparation of Single-Component Adhesive
Vulcanizing fluid 760 (cement)
Cushion Gum
toluene
SCA wet blend toluene
SCA wet toluene
Vulcanizing fluid 760 (cement)
Cushion Gum
SCA dry blend
SCA dry
SCA dry blend low cement
SCA dry low cement
SCA Preparation

## Slide 5: Laminate Preparation I
Vulcanizing fluid 760 (cement)
Cushion Gum
TCA laminate prep 2 kg solids/m2
F3 cured
Cushion Gum
CG only laminate prep
F3 cured
Vulcanizing fluid 760 (cement)
Cement only laminate prep
F3 cured
Laminate image
TCA lam peel test
CG only lam peel test
Cement only lam peel test
No adhesive laminate prep
F3 cured
No adhesive lam peel test
Laminate Adhesion Strength

## Slide 6: Laminate Preparation II
SCA wet toluene
SCA wet lam prep 0.33 kg solids/m2
F3 cured
SCA wet lam peel test 0.33 kg solids/m2
SCA wet toluene
SCA wet lam prep 0.67 kg solids/m2
F3 cured
SCA wet lam peel test 0.67 kg solids/m2
SCA wet toluene
SCA wet lam prep 1 kg solids/m2
F3 cured
SCA wet lam peel test 1 kg solids/m2
SCA wet toluene
SCA wet lam prep 2 kg solids/m2
F3 cured
SCA wet lam peel test 2 kg solids/m2
SCA wet toluene
SCA evap lam prep 2 kg solids/m2
F3 cured
SCA evap lam peel test 2 kg solids/m2
Laminate Adhesion Strength

## Slide 7: Laminate Preparation III
SCA dry
SCA dry lam prep 0.89 kg solids/m2
F3 cured
SCA dry lam peel test 0.89 kg solids/m2
SCA dry
SCA dry lam prep 13.6 kg solids/m2
F3 cured
SCA dry lam peel test 13.6 kg solids/m2
SCA dry
SCA dry lam prep 14.6 kg solids/m2
F3 cured
SCA dry lam peel test 14.6 kg solids/m2
SCA dry
SCA dry lam prep 15.5 kg solids/m2
F3 cured
SCA dry lam peel test 15.5 kg solids/m2
SCA dry
SCA dry lam prep 19.8 kg solids/m2
F3 cured
SCA dry lam peel test 19.8 kg solids/m2
Laminate Adhesion Strength

## Slide 8: Recycled Rubber Preparation
F3 GRP
SCA dry
Coating of GRP X
Pretreatment of cGRP X
Reblending of cGRP X
Curing of cGRP X
F3 uncured
Recycled rubber X
Die cutting X
Tensile test X
SCA dry low cement
This graph must be recreated 32 times with X = all possible 5-digit binary numbers i.e. 10110 or 00111. For all 16 of the numbers starting in 0, use “SCA dry” as the material input. For all 16 numbers starting in 1, use “SCA dry low cement” as the input. F3 GRP and F3 uncured remain unchanged between the graphs.
Factorial Design with Controls

## Slide 9: Recycled Rubber Controls
Reblending of cGRP base control
Curing of cGRP base control
F3 uncured
Recycled rubber base control
Die cutting base control
Tensile test base control
F3 GRP
Reblending of cGRP negative control
Curing of cGRP negative control
F3 uncured
Recycled rubber negative control
Die cutting negative control
Tensile test negative control
Reblending of cGRP trial control
Curing of cGRP trial control
F3 uncured
Recycled rubber trial control
Die cutting trial control
Tensile test trial control
Factorial Design with Controls

## Slide 10: What About Data Analysis?
Tensile test 00000
Tensile test 00001
Tensile test 00010
Tensile test 00011
Tensile test 00100
Tensile test 00101
Tensile test 00110
Tensile test 00111
Tensile test 01000
Tensile test 01001
Tensile test 01010
Tensile test 01011
Tensile test 01100
Tensile test 01101
Tensile test 01110
Tensile test 01111
Analysis of Factorial Design
Effect Factors
Analysis of Factorial Design
These data are not in this experiment.
Tensile test 10000
Tensile test 10001
Tensile test 10010
Tensile test 10011
Tensile test 10100
Tensile test 10101
Tensile test 10110
Tensile test 10111
Tensile test 11000
Tensile test 11001
Tensile test 11010
Tensile test 11011
Tensile test 11100
Tensile test 11101
Tensile test 11110
Tensile test 11111

## Slide 11: Inventory I
Vulcanizing fluid 760 (cement)
Cushion Gum
Rubber Formulation Ingredients
Stearic acid
Carbon black N330
High-cis polybutadiene
Zinc oxide
BHT
TBBS
sulfur
toluene
F3 masterbatch
F3 uncured
F3 cured
F3 GRP

## Slide 12: Inventory II
Recycled Rubbers
Recycled rubber 00000
Recycled rubber 00001
Recycled rubber 00010
Recycled rubber 00011
Recycled rubber 00100
Recycled rubber 00101
Recycled rubber 00110
Recycled rubber 00111
Recycled rubber 01000
Recycled rubber 01001
Recycled rubber 01010
Recycled rubber 01011
Recycled rubber 01100
Recycled rubber 01101
Recycled rubber 01110
Recycled rubber 01111
Recycled rubber 10000
Recycled rubber 10001
Recycled rubber 10010
Recycled rubber 10011
Recycled rubber 10100
Recycled rubber 10101
Recycled rubber 10110
Recycled rubber 10111
Recycled rubber 11000
Recycled rubber 11001
Recycled rubber 11010
Recycled rubber 11011
Recycled rubber 11100
Recycled rubber 11101
Recycled rubber 11110
Recycled rubber 11111
Recycled rubber base control
Recycled rubber negative control
Recycled rubber trial control